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Product: 75W-90 GL-5
[bookmark: _GoBack]Type: LS Synthetic Gear Oil
________________________________________________________________
 
Why Use Driven Racing Oil?
Born from Joe Gibbs Racing, Driven Racing Oil is formulated specifically for high performance applications. Utilizing the latest in synthetic oil technology, Driven gear oils provide cutting edge performance that is trusted by professional racing teams around the world. Driven’s unique technology reduces operating temperature and friction, which means more efficient power transfer and longer gear life.
    
Is This The Right Oil For My Application?
Driven Racing Oil 75W-90 GL5 synthetic gear oil is designed to provide the highest level of protection in high speed and load environments. Driven 75W-90 is compatible with hypoid and straight cut gears as well as open differentials, Torsen style differentials and Detroit locker differentials. Driven recommends the use of Driven Gear Break-In oil prior to using the 75W-90 gear oil if the gears have not been polished.

75W-90 GL-5 Synthetic Gear Oil Product Information

Product Type: Gear Oil – Synthetic 
SAE Grade: 75W-90

Typical Physical Characteristics
	PARAMETER
	TEST METHOD
	VALUE

	HTHS
	ASTM D5481
	4.9

	Viscosity at 40°C. cSt
	ASTM D445
	92

	Viscosity at 100°C, cSt
	ASTM D445
	14.8

	Sulfur
	ASTM D6481
	1.678

	Phos
	ASTM D6481
	1300ppm (.131%)
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